## Slide 1: Synthesis of EAP actuator
Inna Baranova,
Fred Elhi,
Robert Valner

## Slide 2: Initial setup
Synthesized an EAP actuator.
Precut PVdF strip.
Synthesis with pyrrole and sodium dodecylbenzenesulfonatein (NaDBS) in 0,1 M sodium carbonate.

## Slide 3: Synthesis
Two electrode system.
20 sec for 1 polymerisation.
Synthesis for ~ 5 h in ethylene glycol in PARSTAT.

## Slide 4: Polymerization
Chart: Potential (V) change in time (s)

## Slide 5: Delamination

## Slide 6: Force measurements
Polypyrrole triflate PVdF actuator.
Measurements in 0,1 M propylene carbonate triflate.
Dimensions of the actuator:
2,5 mm x 19 mm
Notes: TF – tereftalaat, triflaat ?

## Slide 7: Cyclic voltammetry
Chart: Force (mg) in time (s) 0,650 V to -0,600 V, 5 mVs for 3 cycles

## Slide 8: Chronopotentiometry
Chart: Force (mg) in time (s) 12 microA, 3 cycles

## Slide 9: Chronoamperometry
Chart: Force (mg) in time (s) 0,650 V, 3 cycles

## Slide 10
Thank you for your attention!