## Slide 1
MD Simulations of Fe Precipitates in Cu
x
z
Voids near the surface act as stress concentrators in a high external electric field. They are nucleation centers for dislocations that lead to stable protrusions on the surface. [3]
Simon Vigonski1, Vahur Zadin1, Alvo Aabloo1, Flyura Djurabekova2
1 Institute of Technology, University of Tartu
2 University of Helsinki
Correspond to: simon.vigonski@ut.ee
This research was supported by the Estonian Science Foundation grant PUT57, CERN+ anything else?
Conclusions
Box dimensions: 186x193x199 Å
Cu <110> direction in z
Various r and h
Motivation
Setup
Frequent vacuum break-downs in CLIC accelerating structures are presumably caused by field-enhancing emitters appearing on the surface. The origin of these emitters is hypothesized to be caused by plastic deformations and dislocations [1]. We investigate the effect of voids and precipitates on dislocation nucleation.
Methods
Near-surface voids
Fe precipitates in Cu
32 ps at 22.8 GV/m
Continually ramping the electric field was found to create a void below the precipitate. The conditions correspond to a long-lasting or cyclic electric field. FEM simulations show that the stress is highest below the Fe precipitate, explaining the possibility of formation of a void there.
Classical molecular dy-namics with LAMMPS, using the Bonny et al. many-body EAM poten-tial. [2]
[1] Timko, H., Modelling vacuum arcs : from plasma initiation to surface interactions, Helsinki University Printing House (2011).
[2] Bonny, G., Pasianot, R. C., Castin, N., Malerba, L., Philos. Mag. 89, 3531–3546 (2009).
[3] Pohjonen, A. S., Parviainen, S., Muranaka, T., Djurabekova, F., J. Appl. Phys. 114, 033519 (2013).
Extensive stacking faults are observed in the presence of large Fe precipitates close to the surface. A depression tends to form on the surface, creating a Cu-Fe-vacuum interface and facilitating atom evaporation.
Inserting Fe as an irregular sphere and relaxing the system causes a knot of Cu stacking faults to form around the precipitate even without an external electric field.
Irregular precipitates
Precipitates adjacent to the surface facilitate vaporization
Voids can appear below the precipitate under certain conditions.
Irregular precipitates offer more dislocation nucleation sites
Fixed boundary
r
h
Force
Cu
Fe
E = 29.4 GV/m
E = 29.8 GV/m
E = 30.0 GV/m
E = 30.1 GV/m
E = 30.6 GV/m
Small voids start to form and grow
The small voids combine into a large void
FEM pic here
112 ps at 22.8 GV/m
Cu atoms in a perfect lattice not shown.
Stress concentrations in Cu and electric field strength near the surface from FEM simulations.
Stacking faults in Cu around a void from MD simulations [3].
Cu atoms in a perfect lattice not shown.