## Slide 1
MD simulations of Fe precipitates in Cu
x
z
The Fe precipitate was set on the boundary of two Cu grains, with <110> and <001> crystal directions in z. The <110> grain was exposed to the surface.
Simon Vigonski1, Vahur Zadin1, Alvo Aabloo1, Flyura Djurabekova2
1 Institute of Technology, University of Tartu
2 University of Helsinki
Correspond to: simon.vigonski@ut.ee
This research was supported by the Estonian Science Foundation grant PUT57, CERN+ anything else?
Conclusions
Box dimensions: 186x193x199 Å
Cu <110> direction in z
Various r and h
Motivation
Setup
Frequent vacuum break-downs in CLIC accelerating structures are presumably caused by field-enhancing emitters appearing on the surface. The origin of these emitters is hypothesized to be caused by plastic deformations and dislocations [1]. We investigate the effect of Fe precipitates on dislocation nucleation.
Methods
Grain boundary
Fe precipitates in Cu
32 ps at 22.8 GV/m
Continually ramping the electric field was found to create a void below the precipitate. The conditions correspond to a long-lasting or cyclic electric field. FEM simulations show that the stress is highest below the Fe precipitate, explaining the possibility of formation of a void there.
Classical molecular dy-namics with LAMMPS, using the Bonny et al. many-body EAM poten-tial. [2]
[1] Timko, H., Modelling vacuum arcs : from plasma initiation to surface interactions, Helsinki University Printing House (2011).
[2] Bonny, G., Pasianot, R. C., Castin, N., Malerba, L., Philos. Mag. 89, 3531–3546 (2009).
Extensive stacking faults are observed in the presence of large Fe precipitates close to the surface. A depression tends to form on the surface, creating a Cu-Fe-vacuum interface and facilitating atom evaporation.
Inserting Fe as an irregular sphere and relaxing the system causes a knot of Cu stacking faults to form around the precipitate even without an external electric field.
Irregular precipitates
Precipitates adjacent to the surface facilitate vaporization.
Voids can appear below the precipitate under certain conditions.
A grain boundary may offer sites for preferential surface geometry change.
Irregular precipitates offer more dislocation nucleation sites.
Fixed boundary
r
h
Force
Cu
Fe
E = 29.4 GV/m
E = 29.8 GV/m
E = 30.0 GV/m
E = 30.1 GV/m
E = 30.6 GV/m
Small voids start to form and grow
The small voids combine into a large void
FEM pic here
112 ps at 22.8 GV/m
Cu atoms on a perfect lattice not shown.
Cu atoms on a perfect lattice not shown.
Ramping the electric field causes stacking faults to develop in two different planes. No stacking faults appear in the <001> grain. Atoms start evaporating at the surface grain boundary.
E= 25.6 GV/m