## Slide 1: Basic physics experiments for benefit of cancer research: research on materials for linear accelarators in CERN
University of Tartu:
V. Zadin
A. Aabloo
University of Helsinki:
A. Pohjonen
S. Parviainen
F. Djurabekova
CERN:
W. Wuench
M. Aicheler
2013
IMS Lab

## Slide 2: Outline
What is a linear accelerator and CLIC
Electrical breakdowns
Multiscale material simulations
Medical applications of linear accelerators

## Slide 3: Compact Linear Collider
Two-beam-acceleration concept: The 12 GHz RF power is generated by a high current electron beam (drive beam) running parallel to the main beam.
Drive beam is decelerated in special power extraction structures (PETS) and the generated RF power is transferred to the main beam.
This leads to a very simple tunnel layout without any active RF components
Physics beyond the standard model
Precise measurements of Higgs boson
Investigation of exotic Higgs interactions
Very „clean“ environment

## Slide 4: CLIC near CERN
Tunnel implementations (laser straight)
Central MDI & Interaction Region

## Slide 5: Electrical breakdown

## Slide 6: Electrical breakdowns in CLIC
Accelerating structure damage due to electrical breakdowns
Local field enhancement up to factor 100
Field enhancement caused by „invisible needles“
Highest RF field gradient
Electrical breakdown rate must be decerased under 310-7 1/pulse/m
Voids in the material as possible factors affecting surface defects
Accelerating el. field 100-150 MV/m
Electrical breakdowns at CLIC accelerator accelerating structure materials
R. Behrisch, Plenum, 1986
B. Jüttner, 1979

## Slide 7: SEM analysis
A. Degiovanni CLIC Workshop 2013

## Slide 8
A. Degiovanni CLIC Workshop 2013

## Slide 9
surface depressions which can be the precursors of the bubble-like craters
projection of molten copper
burst bubble
A. Degiovanni CLIC Workshop 2013

## Slide 10: Computer simulations in Chemistry and Physics
DFT
Molecular dynamics
Mesoscale modeling
Finite Element Analysis
Distance
1Å
1nm
1μm
10nm
1mm
femtosec
picosec
nanosec
microsec
seconds
years
Time

## Slide 11: Material model
Elastoplastic deformation of material, simulation of large strains
Validation of material model and parameters by conducting tensile stress simulations
Accurate duplication of the experimental results (tensile and nanoindentation test)
Parameters from tensile test are macroscopic, single crystal parameters are needed due to large grains in soft copper
 | Structural Steel | Soft Copper (CERN) | Single crystal copper [1] | Often used copper parameters
Young’s modulus | 200 GPa | 3.05 GPa | 57 GPa | 110 GPa
Initial yield stress | 290 MPa | 68 MPa | 98 MPa | 70 MPa
[1] Y. Liu, B. Wang, M. Yoshino, S. Roy, H. Lu, R. Komanduri,J. Mech. Phys. Solids, 53 (2005) 2718

## Slide 12: Initial plastic deformation
the top view and a slice of the system at time t = 114 ps when the first bump has formed

## Slide 13: “Catastrophic”growth of a protrusion at the void
the top view and a slice of the system at time t = 130 ps when the fully developed protrusion is clearly visible.

## Slide 14: MD vs FEM
MD – exaggerated el. fields are needed
MD simulations are accurate, but time consuming
FEM is computationally fast, but limited at atomistic scale
Very similar protrusion shape
Material deformation starts in same region

## Slide 15: Void at max. deformation – different materials
Similar protrusion shape for all materials
Higher el. fields are needed to deform stronger materials
Slightly different maximum stress regions
Plastic deformation distribution highly dependent from material
Stainless Steel
Single crystal Cu
Soft Cu

## Slide 16: Protrusion formation
Scale invariance – larger voids produce only larger protrusions
Well defined protrusion evolves on the steel surface
Low protrusion evolves on the soft copper surface
Protrusion formation on copper surface requires ~2 times lower el. field
Protrusion formation starts after material becomes plastic
Soft copper is „harder“ to deform
  Material hardening around the void
  Nearby material deformation due to low Young modulus
Over 2000 MV/m is required to initiate any significant protrusion formation in soft copper
Soft Cu
Steel

## Slide 17: Effect of void shape
Void formation starts at fields > 400 MV/m
Material is plastic only in the vicinity of the defect
Thin slit may be formed by combination of voids or by a layer of fragile impurities
Field enhancement factor ~2.4
Thin material layer over the void acts like a lever, decreasing the pressure needed for protrusion formation

## Slide 18: Yield point
Nonlinear dependence from the void depth
For h/r<0.3, yielding starts at void tip
For h/r=0.3, yielding equal at tip and sides
For h/r>0.3, stress is carried to the sides of the void
Three deformation mechanisms
  Deformation at metal surface
  Deformation at void surface
  Deformation due to decreased surface area
Too deep void starts to decrease the effective surface area of the sample
Steel
Single crystal copper
Soft copper

## Slide 19: Introduction: the characteristics of therapeutic beams
1. Better depth-dose distribution
2. Charged particles can be steered with magnets
3. Less energy is deposited into the healthy tissue
 SPOT SCANNING
Charged hadron beam that loses energy in matter
27 cm
Tumour
target
200 MeV - 1 nA
protons
4800 MeV – 0.1 nA
carbon ions
(radioresistant tumours)
Depth-dose
distribution
Courtesy of PSI

## Slide 20: Cyclinac = Cyclotron + Linac for hadrontherapy
External pulsed source
High current CYCLOTRON
to the patient
ACTIVE ENERGY MODULATION +
HIGH REP RATE PULSED BEAM
Best suited for treating moving organs with spot scanning technique combinend with 3D feed-back systems and multi-painting
 | Beam always present | Energy variation by electronics means | Time to vary energy
Cyclotron | YES | NO | 50 ms
Synchrotron | NO | YES | 1 s
Cyclinac | YES | YES | 2 ms
LinAc
Notes: In particle physics, a hadron i/ˈhædrɒn/ (Greek: ἁδρός, hadrós, "stout, thick") is a composite particle made of quarks held together by the strong force (in the same way as atoms and molecules are held together by the electromagnetic force).
LinAcc-s are used to produce x-rays as well. Fast deacceleration of electrons.

## Slide 21: High gradients are needed to keep the machine compact
CABOTO:
  Length < 25 m
  Ea > 20 MV/m
TULIP:
  Length < 10 m
  Ea > 20 MV/m
TUrning LInac for Protontherapy
TULIP=

## Slide 22: Summary
High gradients are needed to keep the machine compact
Electrical breakdowns must be under control
Material deformation due to voids
  Protrusion shape is similar for all simulated materials
  Material deformation starts after exceeding yield strength
  Three protrusion generation mechanisms
    Deformation mechanisms change at h/r~0.3 and h/r~ 1
  Too deep void starts to decrease the effective surface area of the sample
New opportunities for radiotherapy (hadron therapy)

## Slide 23: Thank you for your attention!

## Slide 25: Some CLIC facts
Accelerator length 50 km
  Distance between Tartu-Otepää ~41 km
Accelerating field 100-150MV/m
    Electrical breakthrough in air at 3MV/m
    Theoretical electirc breakdown in CLIC ~11-12 GV/m
High elelectric field is needed to minimize the length of the accelerator
  High electric field leads to repeated electrical breakdown problem
Electron-positron beam collisions at the energies from 0.5 TeV to 5 TeV

## Slide 26: …Multiscale/multiphysics computational model to simulate electrical breakdown
Stage 1: Charge distribution @ surface
Method: DFT with external electric field
Stage 4: Plasma evolution, burning of arc
Method: Particle-in-Cell (PIC)
Stage 5: Surface damage due to the intense ion bombardment from plasma
Method: Arc MD
~few fs
~few ns
~ sec/hours
~10s ns
~ sec/min
~100s ns
Stage 2: Atomic motion & evaporation
+
Joule heating (electron dynamics)
Method: Hybrid ED&MD model (includes Laplace and heat equation solutions)
Stage 3b: Evolution of surface morphology due to the given charge distribution
Method: Kinetic Monte Carlo
Stage 3a: Onset of tip growth; Dislocation mechanism
Method: MD, ED+MD, FEM…
R. Behrisch, Plenum, 1986
B. Jüttner, 1979

## Slide 27
Proposal with two treatment rooms

## Slide 28: Properties of the beam of different accelerators
 | Beam always present during treatment | Energy variation by electronics mean | Time needed to vary the energy
Cyclotron | YES | NO | 50 ms (*)
Synchrotron | NO | YES | 1 s
Cyclinac | YES (**) | YES | 2 ms
Cyclinac is best suited for treating moving organs with spot scanning technique combinend with 3D feed-back systems and multi-painting
(*) with fast moving absorbers
(**) rep rate up to 300 Hz