## Slide 1: Finite elements simulations of surface protrusion evolution due to spherical voids in the metals
2013
University of Tartu:
V. Zadin
A. Aabloo
University of Helsinki:
A. Pohjonen
S. Parviainen
F. Djurabekova
CERN:
W. Wuench
M. Aicheler

## Slide 2: Electrical breakdowns
Accelerating structure damage due to electrical breakdowns
Local field enhancement up to factor 100
Field enhancement caused by „invisible needles“
Electrical breakdown rate must be decreased under 310-7 1/pulse/m
Voids in the material as possible factors affecting surface defects
Accelerating el. field 100-150 MV/m
Electrical breakdowns at CLIC accelerator accelerating structure materials
M. Aicheler, MeVArc 2011

## Slide 3: Void hypothesis
Mechanism behind field emitting tip generation
Void in material as stress concentrators
  Spherical voids due to surface energy minimization
  Single void in metal
Several mechanisms acting at once to produce the tip?
Understanding protrusion growth mechanism in the case of spherical void in DC electrical field
  Soft copper
  Single crystal copper
  Stainless steel

## Slide 4: Computer simulations in Chemistry and Physics
DFT
Molecular dynamics
Mesoscale modeling
Finite Element Analysis
Distance
1Å
1nm
1μm
10nm
1mm
femtosec
picosec
nanosec
microsec
seconds
years
Time

## Slide 5: Simulated system
Fully coupled electric field – mechanical interaction
  Electric field deforms sample
  Deformed sample causes local field enhancement
Dc El. field ramped from 0 … 10 000 MV/m
Comsol Multiphysics 4.3
  Nonlinear Structural Materials Module
  AC/DC module
3D-simulations, 2D-snapshots
Simulated materials:
  Soft copper
  Single crystal copper
  Stainless steel

## Slide 6: Material model
Elastoplastic deformation of material, simulation of large strains
Validation of material model and parameters by conducting tensile stress simulations
Accurate duplication of the experimental results (tensile and nanoindentation test)
Parameters from tensile test are macroscopic, single crystal parameters are needed due to large grains in soft copper
 | Structural Steel | Soft Copper (CERN) | Single crystal copper [1] | Often used copper parameters
Young’s modulus | 200 GPa | 3.05 GPa | 57 GPa | 110 GPa
Initial yield stress | 290 MPa | 68 MPa | 98 MPa | 70 MPa
[1] Y. Liu, B. Wang, M. Yoshino, S. Roy, H. Lu, R. Komanduri,J. Mech. Phys. Solids, 53 (2005) 2718

## Slide 7: MD vs FEM
MD – exaggerated el. fields are needed
MD simulations are accurate, but time consuming
FEM is computationally fast, but limited at atomistic scale
Very similar protrusion shape
Material deformation starts in same region

## Slide 8: Void at max. deformation – different materials
Similar protrusion shape for all materials
Higher el. fields are needed to deform stronger materials
Slightly different maximum stress regions
Plastic deformation distribution highly dependent from material
Stainless Steel
Single crystal Cu
Soft Cu

## Slide 9: Protrusion formation
Scale invariance – larger voids produce only larger protrusions
Well defined protrusion evolves on the steel surface
Low protrusion evolves on the soft copper surface
Protrusion formation on copper surface requires ~2 times lower el. field
Protrusion formation starts after material becomes plastic
Soft copper is „harder“ to deform
  Material hardening around the void
  Nearby material deformation due to low Young’s modulus
Over 2000 MV/m is required to initiate any significant protrusion formation in soft copper
Soft Cu
Steel

## Slide 10: Protrusion formation at different depths
Close to surface void needs smallest el. field for deformation
Max. stress for near surface voids is concentrate between void and sample surface
Max. stress distribution moves to the sides of void by increasing depth
Deeper voids cause whole material to deform plastically
Soft Cu

## Slide 11: Field enhancement factor
Field enhancement factor to characterize protrusions shape
Soft copper
  Elastic deformation affects field enhancement
  Field enhancement increasing over whole el. field range
  Field enhancement is continuous and smooth
Stainless steel, single crystal Cu
  Field enhancement almost constant until critical field value
  Very fast increase of the field enhancement factor
Maximum field enhancement is 2 times
Field enhancement corresponds to protrusion growth
Soft Cu
Steel

## Slide 12: Surface stress distribution
Soft copper
  Continuous stress increase on void and surface
Stainless steel
  Plateau at yield strength
  Material hardening and further plastic deformation
Mayor differences in stress due to Young modulus
Low Young modulus avoids sudden jumps in field enhancement
Deformation mechanism changes at depth~0.3
Soft Cu
Electric field
Steel
h/r= 0.2
h/r= 0.3
h/r= 0.5
h/r= 1

## Slide 13: Yield point
Nonlinear dependence from the void depth
For h/r<0.3, yielding starts at void tip
For h/r=0.3, yielding equal at tip and sides
For h/r>0.3, stress is carried to the sides of the void
Three deformation mechanisms
  Deformation at metal surface
  Deformation at void surface
  Deformation due to decreased surface area
Too deep void starts to decrease the effective surface area of the sample
Steel
Single crystal copper
Soft copper
h/r=0.2

## Slide 14: Deformation at realistic electric field strength
Void formation starts at fields > 400 MV/m
Material is plastic only in the vicinity of the defect
Thin slit may be formed by combination of voids or by a layer of fragile impurities
Field enhancement factor ~2.4
Thin material layer over the void acts like a lever, decreasing the pressure needed for protrusion formation

## Slide 15: Conclusions
FEM is a viable too to simulate material defects
  MD is still needed to determine physics behind the effects
Protrusion shape is similar for all simulated materials
Material deformation starts after exceeding yield strength
Field enhancement corresponds to protrusion growth
Three protrusion generation mechanisms
  Deformation mechanisms change at h/r~0.3 and h/r~ 1
Too deep void starts to decrease the effective surface area of the sample
Single void needs too high el. field to produce a protrusion

## Slide 16: Thank You for Your attention!