## Slide 1
Reliability measurements of Ionic EAP Materials
Andres Punning, Indrek Must, Friedrich Kaasik, Janno Torop, Alvo Aabloo*
IMS Lab, Institute of Technology, University of Tartu, Nooruse 1, 50411 Tartu, Estonia
* Corresponding author (Tel: +3725078356; E-mail: alvo.aabloo@ut.ee)
Outline
Mission of the project
Involved iEAP materials
Test procedure
Test equipment
Acquired data
Performance
Long term degradation of iEAP
2 ways of sudden death
Radiation results
Conclusions
Speculations

## Slide 2
The research is focused on lifetime and reliability of iEAP in the conditions of Low Earth Orbit.
The samples were tested against the following hazardous environments:
Gamma-radiation (Co-60, different doses 400, 1200, 3600 Gy)
X-ray radiation (140 R/min, 120 min)
UV radiation (xenon lamp at 25 cm, 15 days)
Freezing
  boiling nitrogen (77K) 15 days
  boiling helium (4K) 10 minutes
Low atmospheric pressure (1 mbar) 15 days
Notes: doosid

## Slide 3
The experiments involved 7 iEAP materials, significantly different by means of the materials of electrodes, membranes, and electrolyte.
 | Provided By | Membrane | Electrodes | Electrolyte
A | University of Tartu, Estonia | Nafion | CDC+gold | Emi-TF
B | University of Tartu, Estonia | PVDF(HFP) | CDC | EMIBF4
C | AIST, Japan | PVDF(HFP) | CNT | EMIBF4
D | University of Nevada, USA | Nafion | Pd+Pt | Water+Na+
E | Université de Cergy-Pontoise, France | PVDF(HFP) | Ppy | EMITFSI
F | University of Wollogong, Australia | PVDF(HFP) | Au+Ppy | PC+LiTFSI (0.1M)
G | University of Tartu, Estonia | PVDF(HFP) | Ppy | PC+LiTFSI (1.0M)
A: doi:10.1088/0964-1726/18/9/095028
B: doi:10.1016/j.carbon.2011.03.034
C: doi:10.1016/j.electacta.2008.02.113
D: doi:10.1088/0964-1726/17/3/035011
E: doi:10.1016/j.synthmet.2003.10.005
F: doi:10.1016/j.synthmet.2006.06.022
G: doi:10.1016/j.snb.2012.01.075

## Slide 4
60 identical samples
5 x 20mm
Test procedure
Notes: doosid

## Slide 5
60 identical samples
5 x 20mm
Divided into portions ~7-10pcs
.......
Test procedure
reserve
Notes: doosid

## Slide 6
60 identical samples
5 x 20mm
Divided into portions ~7-10pcs
.......
reserve
UV radiation
X-ray radiation
Gamma radiation
Etc.
Only one type of radiation applied to each portion
Test procedure
Notes: doosid

## Slide 7
60 identical samples
5 x 20mm
Divided into portions ~7-10pcs
.......
reserve
UV radiation
X-ray radiation
Gamma radiation
Etc.
Only one type of radiation applied to each portion
One portion kept in ideal conditions
Test procedure
Notes: doosid

## Slide 8
One portion kept in ideal conditions
Only one type of radiation applied to each portion
60 identical samples
5 x 20mm
Divided into portions ~7-10pcs
.......
reserve
UV radiation
X-ray radiation
Gamma radiation
Etc.
Performance decrease rate of all samples in identical conditions
Test procedure
What we expected
Notes: What expected: that some radiation increases the degradation rate
But maybe some radiation improves the material
Speculation: vacuum improves a bit the dry iEAP materials

## Slide 9
One portion kept in ideal conditions
Only one type of radiation applied to each portion
60 identical samples
5 x 20mm
Divided into portions ~7-10pcs
.......
UV radiation
X-ray radiation
Gamma radiation
Etc.
Performance decrease rate of all samples in identical conditions
Test procedure
What we expected
performance
measured once, this gives degradation in time
reserve
Notes: Lõpus mõõdetakse reserv üle, et teada saada degradeerumist ajas

## Slide 10
Time schedule
Time (days)
0
Performance test 0
60
Performance test 1
120
Performance test 2
Performance test 3
Performance test n-1
Performance test n
Damage
Performance test n+1
.....
Each sample passed the following procedure:
1-4 weeks
1 week
Each performance test of a sample includes
attaching it to electrical contacts
applying complex voltage signal
observation of electric current and amplitude of bending up to a few minutes
End of test was decided on the fly, while n reached ~ 103 ... 104
The same procedure should be performed with the remaining five hundreds of samples ...

## Slide 11
For this purpose a special conveyor was developed,
continously repeating the test with 4 x 60 samples.
4 floors,
Each floor:
1 sample tested with camera
1 sample tested with force sensor
58 samples under training
FLOOR4
FLOOR3
FLOOR2
FLOOR1
FLOOR4 CAMERA
FLOOR3 CAMERA
FLOOR2 CAMERA
FLOOR1 CAMERA
FLOOR4 FORCE SENSOR
FLOOR3 FORCE SENSOR
FLOOR2 FORCE SENSOR
FLOOR1 FORCE SENSOR

## Slide 12
Process of measurement consists of two types of cycles: training cycles and measurement cycles.
measurement
training
Each sample tested in every 29 x 3 bends
Notes: Klõksa vilm käima

## Slide 13
All 4 floors are switched synchronously
FLOOR4 UNDER CAMERA
FLOOR1 FORCE SENSOR
Notes: Klõksa vilm käima

## Slide 14
The „wet“ IPMC
Samples under training are working in solvent baths
Solvent baths

## Slide 15
Testing signal
Frequencies
in this order:
10 Hz
5 Hz
2.5 Hz
1.25 Hz
0.64 Hz
0.32 Hz
0.16 Hz
0.08 Hz
0.04 Hz
1.5 periods each
Signal consists of series sequence of sine signals of different frequencies. Each frequency lasts 3 half periods. The delay between the sequences is at least 0.5 half periods of the previous frequency while the initial phases are opposite.
Notes: The response might be highly nonlinear, therefore the wide spectrum signals, e.g. sweep, white noise, chirp, etc. are unobjectionable. Instead, the exciting signal was a gradual sweep. It consists of series sequence of sine signals of different frequencies. Each frequency lasts 3 half periods. The delay between the sequences is at least 0.5 half periods of the previous frequency while the initial phases are opposite.
Ma alguses lootsin et liigutuse amplituudi sagedussõltuvus vananedes muutub. Tegelt ma lõpuks seda ikkagi ei näe.

## Slide 16
2 causes of degradation
pure temporal degradation
degradation caused by environmental conditions
As the initial object of this project was comparing the degradation rates of irradiated and non-irradiated samples,
we decided to accelerate the degradation by applying the driving voltage close to the maximal
when experiment lasts too long, it is rather impossible to differentiate them
Amplitude of the applied voltage
We did not try to demonstrate that the iEAP materials are capable working centillions of working cycles
It succeeded :)

## Slide 17
Measuring the wide spectrum with the sampling frequency, appropriate to the highest frequency generates too much data, therefora a specialized hardware sync generator was used
This way the 100 seconds signal 10 ... 0.04 Hz generates only 700 points of electrical signal and 165 frames of video
Red – camera sync
Green – DAQ sync
10 Hz signal
Sampling rates of electrical signals and video are different, but knowing exact times enables aligning the two types of data

## Slide 18
Acquired data
The overall object of the project is comparing degradation of damaged and unimpaired samples.
Same procedure is applied to completely different iEAP materials.
Despite the hardware sync, the measurements generate huge amount of data.
We are looking for a minimal set of universal parameters describing the productivity of any sample of any type of involved iEAP materials - Performance
All following examples are based on the iEAP materials, produced by our own,
mostly with PVDF(HFP) membrane, electrodes made of carbide-derived carbon,
and EMIBF4 electrolyte.

## Slide 19
High frequencies
Moderate frequencies
Electrical signals
Measured voltage and electric current show frequency-dependent impedance
Low frequencies
Notes: Mis siit saab

## Slide 20
Same procedure applied to completely different iEAP materials
Laser distance meter
Laser distance meter
Notes: Laseriga saab mõõta ainult väikese painde korral

## Slide 21
Shape of the actuator is characterized by a number of relative angles
Notes: Each next angle along the length of the actuator is relative to the previous one

## Slide 22
Time=0...100 s
Time=11-13 s
Time=16-28 s
Angles of vectors
At high frequencies this iEAP does not bend much.
This graph contains still too much data, we are looking for a single number, describing performance.
Notes: Päris kõrgetel sagedustel see lihas ei tee midagi
Siin on ikka andmeid liiga palju

## Slide 23
Performance : tip absolute angle peak to peak
This parameter is valid until the actuator bends out of the camera’s field of view, and reflects adequately the performance even in the case of considerable initial creep of the sample.
Notes: Performancet näitab peak-to peak kõige madalamal sagedusel

## Slide 24
We define the Performance as:
tip absolute angle peak to peak at slowest frequency
Electric current: peak to peak
Relative angles of the vectors
Tip absolute angle = sum of the vector angles
Next we show that during degradation
tip absolute angle peak to peak
and electric current: peak to peak show similar trends
Notes: Nüüd on meil vool ja performance, need on väga sobivad parameetrid
Alumine pilt on ülemiste joonte summa

## Slide 25
Force measurement
It may seem that measuring the blocking force is the easiest way to estimate the performance of an actuator, as the output is a single continous electrical signal.
adjusting the force sensor to an actuator is a delicate task. Especially, when the sample suffers from creep, it is impossible to push it to the force gauge with zero initial force, or without breaking the sample.
This type of measurement was initially planned to the equipment, but the results are inconsistent and erratic.
Notes: It may seem that measuring the blocking force is the easiest way to estimate the performance of an actuator, as the output is a single continous electrical signal. Nevertheless, adjusting the force sensor to an actuator is a delicate task. Especially, when the sample suffers from creep, it is impossible to push it to the force gauge with zero initial force, or without breaking the sample. This type of measurement was initially planned to the equipment, but the results are inconsistent and erratic.

## Slide 26
Long-term degradation of the iEAP actuators.
electric current and performance vs. performed cycles of actuation vs. the time passed from the first actuation.
Trends of current and performance are pretty similar
Notes: the electric current and performance vs. performed cycles of actuation as well as vs. the time passed from the first actuation.
We can see that the trends of electric current and performance are pretty similar.
Seepärast saab estimeerida vananemist jälgides voolu (elektriliselt mõõdetav).

## Slide 27
2 ways of sudden death: 1 – No contact
Notes: Ometi on peale lihtsa vananemise 2 sorti äkksurma: kontakti puudumine, tavaliselt delamineerub

## Slide 28
2 ways of sudden death: 2 – shorting
Notes: Ja lühis

## Slide 29
Post-mortal respawn
Notes: Oleme näind ka elluärkamist

## Slide 30
NONE
UV
Gamma
77K
X-Ray
Vacuum
Radiation results
Notes: Ükski kiiritus ei tapa,
igaühest mõni sureb enneaegu ära,
alg-performanced on väga erinevad
ja sampleid on liiga vähe et mingitki statistikat teha

## Slide 31
One interesting result with Ppy actuators (died too fast)
Tests conducted continously:
Capable making
3000 bends in 10 hours
Tests conducted with 1 hour delays:
Capable making
only 400 bends in 36 hours
In our test the delay was 2.5 hours,
Most of samples were dead after 10 tests (~100 bends) only :(

## Slide 32
Conclusions
None of the tested radiations/levels do not destruct completely any of the tested iEAP materials
The most harmful is UV radiation
Degradation depends on time and performed cycles
Notes: Time-dependent degradation process starts with the first use
See tähendab
nigu proovid kas käib, hakkab degradeerumine pihta
Ja selleks ajaks kui tegelt vaja on, on juba palju kehvem
Kui ei proovi kas käib, siis võib juhtuda et tegeliku vajaduse korral peab palju rohkem vastu
(muidugi juhul kui ei olnud ebaõnnestunud tükk)

## Slide 33
Speculations
Degradation and lifetime of the iEAP materials depend on
  Applied voltage amplitude
  Storage conditions
  Utilization regime (signal shape, frequencies, delays, etc.)
Time-dependent degradation process starts with the first use
Vacuum improves the performance of dry IL-containing iEAP materials
Difficult to fabricate exactly similar samples
etc...
Demand on standardized procedure
and parameters
This work produced more questions than answers
Notes: Storage conditions – teised autorid on raporteerinuds palju pikemaid eluigasid

## Slide 34
Project team:
IMS Lab research group in University of Tartu, Institute of Technology http://ims.ut.ee
People:
Alvo Aabloo, Urmas Johanson, Andres Punning, Tarmo Tamm, Karl Kruusamäe, Indrek Must, Pille Rinne, Inga Põldsalu, Veiko Vunder, Janno Torop, Rauno Temmer, Friedrich Kaasik, Tõnis Lulla et al.

## Slide 35
This page intentionally left blank

## Slide 36
Notes: Mitut moodi suremise pildid tagavaraks

## Slide 37
3 impedances
do not show much
Notes: Impedantsid ei näita suurt midagi, seepärast ma praegu kratsisin nad välja

## Slide 38
Shape of the actuator is characterized by a number of angles
Notes: Each next angle along the length of the actuator is relative to the previous one

## Slide 39
Xenon lamp
Notes: UV lambi spekter